## Slide 1: DENTAL WAXES

## Slide 2: DEFINITION
variety of natural waxes and resins have been used in dentistry for specific and well defined applications
Waxes are thermoplastic materials which are solids at room temperature but melt without decomposition to form mobile liquids

## Slide 3: CLASSIFICATION OF DENTAL WAXES
Pattern waxes:
Inlay wax
Casting wax
Base plate wax
Wax rim
Shellac denture bas

## Slide 4
Processing wax
Sticky wax
Utility wax
Block-out wax
Boxing & beading wax

## Slide 5
Impression wax
Corrective wax
Bite registration

## Slide 6: Inlay wax
It is a type of pattern wax
Various colors ( blue, green, purple)
Available in sticks, cakes, blocks

## Slide 7: Composition
Paraffin wax: 60%
Carnuaba wax: 20%
Ceresin wax: 10%
Bees wax: 5%
Gum dammar wax: 5%

## Slide 8: Uses of inlay wax
1) It is used to make patterns for metallic restorations.
2) Patterns for inlays
3) Crowns and bridges is first made in wax and then converted into metal or ceramic by casting.

## Slide 10: Casting wax
It is a type of pattern wax.
The pattern for the metallic framework of removable partial dentures and other similar structures is fabricated from casting waxes
These waxes are available in the form of sheets, usually of 28- and 30-gauge

## Slide 12: Base plate wax
It is a type of pattern wax.
Available in thin sheet and sticks ( pink or red )
Mouldable at room temp

## Slide 13: Uses
Used mainly in preparing wax patterns for dental prosthesis.

## Slide 14: Wax rim (bite rim)
It is a type of pattern wax.
Restoring the occlusal relationship
Arrangement of teeth.

## Slide 16: Shellac denture base
It is a type of pattern wax
Wax like resin stable at mouth temp.
It has high softening temperature than other waxes.
It is used as a temporary denture

## Slide 18: Processing wax
Sticky wax:
It is a type of processing wax
If movement occurs the wax tends to fracture than distort.
At room temperature the wax is brittle and breaks easily

## Slide 19: Uses
It is used to align fractured parts of acrylic dentures .
It is used to align fixed partial denture units before soldering .
It is used to seal a plaster splint to the stone cast during

## Slide 20: UTILITY WAX
It is a type of processing wax
Supplied as : It is available in the form of sticks and sheets. Orange or dark red in color.
In orthodontics, periphery wax is white in color

## Slide 21: Uses
May be used on the lingual portion of a bridge pontic to stabilize it while a labial plaster splint is poured

## Slide 22: Boxing & beading waxes
It is a type of processing wax.
Uses:
Beading wax is adapted around the impression borders to create the land area of the cast
Boxing wax is used to build up vertical walls around the impression in order to pour the gypsum product to make a cast base.

## Slide 24: Block out wax
It is a type of processing wax.
Used for filling the undercut area on the cast during processing of the Cr-Co frame work

## Slide 25: Impression waxes
Corrective wax:
Wax in combination with resins of low melting point can be used in corrective impression technique in partial and complete denture prosthesis
Availability: sheets
Used to restore the selected region in the edentulous patients to reproduce the details of mucous membrane

## Slide 26: Bite registration wax
It is used to record the relationship of the upper
& lower teeth in dentulous patients

## Slide 28
Thank you